## Slide 1
 | Gui-Rong Zhang,1 Thomas Wolker,1 Daniel J.S. Sandbeck,2 Macarena Munoz,3 Karl J. J. Mayrhofer,2 Serhiy Cherevko,2 Bastian JM Etzold1,*
Electrochemistry 2018 - Electrochemical Surface Science: From Fundamentals to Applications, Sep. 24 – 26, 2018, Ulm
References:
[1] U. Kernchen, B.J.M. Etzold, W. Korth, et al, Chem. Eng. Technol., 2007, 30, 985
[2] G.R. Zhang, M. Munoz, B.J.M. Etzold, ACS Appl. Mater. Interfaces, 2015, 7, 3562
[3] G.R. Zhang, M. Munoz, B.J.M. Etzold, Angew. Chem. Int. Ed., 2016, 55, 2257
[4] G.R. Zhang, T. Wolker, D. Sandbeck, et al., ACS Catal., 2018, 8, 8244
Solid Catalyst with Ionic Liquid Layer (SCILL) concept
Tuning the Electrocatalytic Performance of Ionic Liquid Modified Pt Catalysts for Oxygen Reduction Reaction via Cationic Chain Engineering
Modifying Pt catalysts using hydrophobic ionic liquids (ILs) has been demonstrated as a facile approach to boosting the performance of Pt catalysts for ORR. This work aims to deepen the understanding and initiate a rational molecular tuning of IL for improved activity and stability. To this end, Pt/C catalysts were modified using a wide variety of [CnC1im][NTf2] ILs with varying alkyl chain lengths in imidazolium cations, and their electrocatalytic properties were systematically investigated. It is disclosed that the catalytic activity strongly correlates with the alkyl chain length of cations, and a distinct dependence of intrinsic activity on the alkyl chain length with the maximum activity obtained on the Pt/C-[C4C1im][NTf2] was identified. The optimum arises from the counterbalance between more efficient suppression of oxygenated species formation on Pt surfaces and more severe passivation of Pt surfaces with elongation of the alkyl chain length in imidazolium cations. Moreover, the presence of IL can also improve the electrochemical stability of Pt catalysts by suppressing the Pt dissolution.
Materials
Catalyst: 20 wt.% Pt/C (HiSpec 3000)
Pt/C
Porous network
Pt/C-SCILL
Modified with
Ionic Liquid
ILs:
Stability testing conditions: 0.4 to 1.1 V in O2-saturated 0.1 M HClO4, 2000 cycles, 1 V s-1
Proposed structure of ILs on Pt surface
The IL helps improve E-Chem stability of Pt/C by suppressing Pt dissolution
Correspondence: Prof. Bastian J.M. Etzold (etzold@tc1.tu-darmstadt.de)
Acknowledgements:
This project has received funding from the European Research Council (ERC) under the European Union's Horizon 2020 research and innovation programme (grant agreement n° 681719).
Cationic Chain Engineering
New microenvironment at solid-liquid interfaces
Electrochemical Characterization
Long cationic chain (n > 6) can more efficiently suppress the formation of non-reactive oxygenated species (e.g., OHad), while causes significant loss in ECAS.
Oxygen Reduction Reaction
0.1 M O2-sat. HClO4, room temperature, ORR: 10 mV s-1, 1600 rpm
The maximum activity was obtained on the Pt/C modified using IL with intermediate length alkyl group (C4)
Proper length of the alkyl chain is the key to obtain promising ORR catalyst
Electrochemical Stability
Pt/C
Pt/C
Pt/C
Pt/C
ADT
Pt/C-IL
Pt/C-IL
Pt/C-IL
Pt/C-IL
0.1 M N2-sat. HClO4, room temperature, scan rate: 20 mV s-1
Short chain ILs: coulombic interaction
Long chain ILs: van der waals interaction
ILs on uncharged surface
ILs on positively charged surface
Dynamic structure of IL
Chain length dependent lipid-like bilayer structure
Conclusions
The presence of IL can:
Improve activity and stability of Pt/C catalysts for ORR;
Suppress the formation of nonreactive species on Pt;
Suppress Pt dissolution under E-Chem conditions;
Lead to Pt surface passivation
“To go beyond is as wrong as to fall short”
 Confucius
The chain length matters…
Ernst-Berl-Institut für Technische und Makromolekulare Chemie, TU Darmstadt, 64287 Darmstadt, Germany
HI-ERN (IEK-11), Forschungszentrum Jülich GmbH, 91058 Erlangen, Germany
Chemical Engineering Section, Universidad Autónoma de Madrid, 28049 Madrid, Spain
J003
E-Chem
in situ ICP-MS
Identical
Location TEM