## Slide 1
Preparation and characterization of electrodes for Na-ion batteries: Na2FeP2O7 and Na0.67MnO2
G. Kucinskis1, I. Nesterova1, B. Kruze1, G. Bajars1, D. Erts2, G. Vaivars1
1. Institute of Solid State Physics, University of Latvia 2. Institute of Chemical Physics, University of Latvia
06.07.2022.

## Slide 2: Na2FeP2O7, Na0.67MnO2 and beyond
Na2FeP2O7
Na-rich Na2+xFe4-2x (P2O7)2
Mixed
Na4M3(PO4)2P2O7
Na0.67MnO2
Na0.67NixMn1-xO2
Coated and/or doped Na0.67MO2

## Slide 3: Synthesis of Na2FeP2O7
Kucinskis et al., J. Alloys and Compounds 895 (2022) 162656
Na2CO3
NH4H2PO4
FeC2O4·2 H2O
(C₆H₁₂O₆)
Mix in DI H2O,
Evaporate H2O
Dry in vacuum oven
3 h
350 °C
Ar/H2 (95:5)
Grind, press pellets
6 h
600 °C
Ar/H2 (95:5)

## Slide 4: Structural/Compositional Characterization
Mix of disordered and graphitic carbon, no significant impurities, only Fe2+, traces of Na2CO3 on the surface
Na2FeP2O7/C
Na2FeP2O7
Presence of carbon source reduces grain size ca. 10x

## Slide 5: Na2FeP2O7: Low Coulombic Efficiency?
1 M NaClO4 in PC
Low Coulombic Efficiency at low rates

## Slide 6: Na2FeP2O7: Low Coulombic Efficiency?
1 M NaClO4 in PC
Low Coulombic Efficiency at low rates
Kim et al., Adv. Funct. Mater. 23, (2013), 1147
Kosova et al., Electrochimica Acta 235 (2017) 42
Similar examples by others
Chen et al., J. Power Sources 246 (2014) 783
Shakoor et al., PCCP 18 (2016) 3929
Gond et al., J. Solid State Chem. 277 (2019) 329

## Slide 7: Na2FeP2O7: Stabilizing SEI is important
1 M NaClO4 in PC
1 M NaClO4 in PC with 5 wt.% FEC
Notes: FEC stabilizes SEI by decomposing and formation of NaF, hence preventing the decomposition of liquid electrolyte and PVDF

## Slide 8: Electrochemical cell
Cathode
Electrolyte
Anode
Interface
Interface

## Slide 9: Na2FeP2O7: Electrochemical Performance
Adding a source of carbon improves electrochemical performance
4.8 wt.% carbon was most optimal carbon content
Ca. 30 % carbon from glucose is converted to carbon additive/coating
Excellent cyclability, no capacity loss over 500 cycles at 1 C

## Slide 10: Na2FeP2O7: Stability in Water (preliminary)
Change in intensities of some peaks, generally reduced peak intensity
Capacity reduced by over two orders of magnitude
Despite being reported in literature (DOI: 10.1039/C3RA47560C) Na2FeP2O7 has turned out to be unstable in water
Chart: Cycle No.
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40
NFP/C(4,8%) charge | 93.5645 | 94.4553 | 93.4799 | 93.2168 | 92.7827 | 92.2054 | 90.795 | 90.7992 | 91.163 | 91.1437 | 90.3339 | 88.0167 | 87.9489 | 87.8333 | 87.7296 | 86.263 | 83.5847 | 83.6769 | 83.7574 | 83.7833 | 81.7794 | 77.85 | 78.1288 | 78.0997 | 78.2663 | 73.4291 | 66.6864 | 66.0304 | 66.2107 | 66.4809 | 61.6684 | 55.0553 | 55.0443 | 55.44 | 55.8791 | 49.8723 | 42.9271 | 42.8329 | 43.1208 | 43.3952
NFP/C(4,8%) discharge | 92.6726 | 92.4325 | 92.5201 | 92.393 | 92.2301 | 90.3334 | 90.3158 | 90.7485 | 90.7824 | 90.8345 | 87.8514 | 87.7721 | 87.6584 | 87.5663 | 87.4714 | 83.4491 | 83.4838 | 83.5521 | 83.6345 | 83.7546 | 77.5462 | 77.8539 | 77.8236 | 77.991 | 77.9868 | 66.3798 | 65.9028 | 66.1145 | 66.3892 | 66.7143 | 54.6962 | 54.9948 | 55.4382 | 55.8933 | 56.2004 | 42.3595 | 42.6944 | 43.0806 | 43.3686 | 43.5833
NFP/C(4,8%) 24 h in water charge | 4.2852 | 2.0733 | 1.8825 | 1.7691 | 1.6911 | 0.82758 | 0.66439 | 0.6529 | 0.64905 | 0.64912 | 0.28666 | 0.21401 | 0.21041 | 0.20952 | 0.20842 | 0.12172 | 0.097792 | 0.095773 | 0.094877 | 0.09463 | 0.051974 | 0.046486 | 0.045939 | 0.045735 | 0.045584 | 0.026988 | 0.024916 | 0.024511 | 0.024353 | 0.024247 | 0.018114 | 0.016878 | 0.016502 | 0.016288 | 0.016125 | 0.011178 | 0.010318 | 0.0098884 | 0.0096734 | 0.0094582
NFP/C(4,8%) 24 h in water discharge | 1.5028 | 1.4864 | 1.4674 | 1.4514 | 1.446 | 0.61336 | 0.62414 | 0.62829 | 0.63178 | 0.63404 | 0.20822 | 0.21255 | 0.21455 | 0.21444 | 0.21413 | 0.10357 | 0.10265 | 0.10186 | 0.10119 | 0.10085 | 0.053372 | 0.052922 | 0.052503 | 0.052117 | 0.051817 | 0.030405 | 0.029977 | 0.029658 | 0.029522 | 0.029335 | 0.020571 | 0.020249 | 0.020035 | 0.019875 | 0.019768 | 0.012095 | 0.011881 | 0.011667 | 0.01156 | 0.01156
1 week
24 h

## Slide 11: Na2FeP2O7: Electrochemical Performance
Minor phase transitions might be taking place during cycling

## Slide 12: Na0.67MnO2: Electrochemical performance (cyclability, 1C)
1 M NaClO4 in PC
1 M NaClO4 in PC with 5 wt.% FEC

## Slide 13: Na0.67MnO2: electrode preparation
Electrode composition: Na0.67MnO2 (75 wt.%), carbon black (15 wt.%), binder (10 wt.)
Notes: DMF for TBA alg

## Slide 14: Synthesis of Na0.67MnO2
Na2CO3
Mn2O3
24 h
900 °C
Air
Press pellets
Kucinskis et al., Batteries 8 (2022) 6

## Slide 15: Morphology of Na0.67MnO2
SEM images indicate a grain size of 1–5 μm

## Slide 16: Na0.67MnO2: Electrochemical Performance
TBA alginate provides the best absolute capacity and a rate capability similar to PVDF
TBA alginate based electrode offers the highest capacity for the first 150 cycles
Na alginate binder based electrode is more stable beyond ca. 150 cycles
1 C

## Slide 17: Na0.67MnO2: Electrochemical performance (cyclability, 1C)
1 M NaClO4 in PC
1 M NaClO4 in PC with 5 wt.% FEC

## Slide 18
Notes: Na alginate – least change

## Slide 19
NaF
C-C
Na2CO3
NaF
Na2CO3
C-H
Na KLL
Na-O-Mn
Notes: Na alginate – least change
NaF, more fluorine in the depth of PVDF and TBA electrodes

## Slide 20: Conclusions and further findings on binders for Na0.67MnO2 and beyond
FEC additive significantly improves SEI stability in Na-ion cells
Na0.67MnO2 is unstable in water (did not affect cyclability, only discharge capacity in this work)
Na alginate binder might stabilize the SEI
Electrode preparation with alginates is very challenging
TBA alginate does not improve electrochemical performance of LiFePO4 electrodes

## Slide 21: Institute of Solid State Physics, Univeristy of Latvia
Team of 20 people working on:
  Electrode materials for Li-ion and Na-ion batteries
  Ageing of Li-ion battery cells
  Catalytic reactions for H2 production
Laboratory of Energy Harvesting and Storage

## Slide 22: THANK YOU!
G. Kucinskis et al., Electrochemical performance of Na2FeP2O7/C cathode for sodium-ion batteries in electrolyte with fluoroethylene carbonate additive, J. Alloys Compounds 895 (2022) 162656
G. Kucinskis et al., Enhanced Electrochemical Properties of Na0.67MnO2 Cathode for Na-Ion Batteries Prepared with Novel Tetrabutylammonium Alginate Binder, Batteries 8 (2022) 6
Project CAMART² at Institute of Solid State Physics, University of Latvia has received funding from the Horizon 2020 Framework Program H2020-WIDESPREAD-01-2016-2017-TeamingPhase2 under grant agreement No. 739508.
G. Kucinskis1, I. Nesterova1, B. Kruze1, G. Bajars1, D. Erts2, G. Vaivars1
1. Institute of Solid State Physics, University of Latvia 2. Institute of Chemical Physics, University of Latvia
gints.kucinskis@cfi.lu.lv
Inovatīvi polimēru un jonu šķidrumu kompozīti nātrija polimēru akumulatoriem lzp-2020/1-0391