## Slide 1: RH plant camera data
Maria Thumfart, Johann Wachlmayr, Christine Gruber (K1-MET GmbH)
Roman Rössler (voestalpine)
Linz, 31.01.2023

## Slide 2: Outline
Motivation
Setup
How to interpret the images
Data set structure
What the data can be used for

## Slide 3: Motivation
RH plant is used to
  reduce content of dissolved gases
  do microalloying
CO2 reduced steel production leads to larger range of different elements in the pig iron  RH will be bottle neck process
Improved process monitoring by image evaluation to detect abnormalities
Blast furnace
BOF
Ruhrstahl Hereaeus degassing
Vacuum degassing
Ladle furnace
Continuous casting
EAF

## Slide 4: Setup
Geometry
  Inner diameter of new vacuum chamber: 1.5m
  Snorkel diameter: 0.4m
  Distance from camera to melt surface 9m
Image data
  Frame rate 1 fps
  1280 x 720 pix
  Jpg colour images
  24 bit
How it works
  Absolute pressure in the chamber = 5mbar  liquid steel sucked into the chamber from ladle
  Argon injected in the left snorkel  circulation of steel induced between ladle and vacuum chamber
camera

## Slide 5: What do we see?
only source of light: thermal radiation
  melt
  refractory walls
brightness reduction due to temperature reduction
specular reflection at the clean steel-offgas-interface  bright rim of dark objects
main parameters for appearance of features:
  temperature
  curvature of the surface
  altitude in the vacuum chamber
other possible explanation: temperature gradient within the objects

## Slide 6: Example images
Empty chamber
Coarse foam during degassing
Droplets during decarbonization
Big structures during decarbonization

## Slide 7: Data set structure
Data structure
  Decarb
    Decarb077
      Empty
      Treatm
    Decarb078
    …
    Decarb090
  Degas
    Degas001
      Empty
      Treatm
    Deags002
    …
    Degas076
The main treatment types in an RH plant are decarbonization and degassing. The first folder contains only images from decarbonisations. The second folder only images from degasings.
Each folder named “empty” contains images from 6.5 min to 4.5 min before the treatment starts. Naming convention emptyXXXX.jpg
Each folder named “treatm” contains images during the treatment labelled as OK by the process data evaluation tool. Naming convention treatmXXXXXX.jpg

## Slide 8: What the data can be used for
The image processing performed within the Inevitable project consists of the following steps:
  Detection of the snorkels in the images of the empty chamber  ROI is chosen as a circle based on their position
  Within the ROI four different texture parameters are calculated
  Based on the time average of all images of one melt the cleanness of the camera lens is evaluated.
  Images with good lens cleanness are used to detect abnormal states during treatments.
The evaluation of the data set showed that the range of observed texture parameters differs between decarbonizations and degassing treatments

## Slide 9: Acknowledgements
K1-MET The authors gratefully acknowledge the funding support of K1-MET GmbH, metallurgical competence center. The research program of the competence center K1-MET is supported by COMET (Competence Center for Excellent Technologies), the Austrian program for competence centers. COMET is funded by the Federal Ministry for Transport, Innovation and Technology, the Federal Ministry for Science, Research and Economy, the province of Upper Austria, Tyrol, and Styria, the Styrian Business Promotion Agency.
SPIRE INEVITABLE INEVITABLE project has received funding from the European Union’s Horizon 2020 research and innovation programme under grant agreement No 869815.

## Slide 10: Thank you